GENERAL REQUIREMENTS

405 DRY-SHAKE FINISH.

Following placing and levelling of the concrete, the floor shall be hardened by the application of Rocland xxxxxsurface hardener, colour xxxxx.

This is to be applied as a dry-shake at the rate of xkg/m2; OR as a wet-on-wet slurry.

The Dry Shake Hardener shall be applied strictly in accordance with the current product technical datasheet, specification and instructions for use by a Rocland approved contractor and shall be finished by repeated passes with a power trowel to provide a fully close dense consistent surface finish. 
The floor shall conform to the requirements of BS2050 for industrial anti-static floors. 
Material requiring site batching shall not be approved. 
The manufacturer shall be registered to ISO 9001 Quality Assurance.

After finishing the power trowelling operation Rocland Ecocure SUPERIOR concrete sealer shall be applied at an application rate of 10 m2 per litre, strictly in accordance with the current product technical datasheet, specification and instructions for use.

The Dry Shake Hardener shall have been tested for abrasion resistance to BS8204: Part 2: 1999 Table 4 Classification of Abrasion Resistance / EN 13892-4; and limiting depths of wear for the accelerated abrasion test and achieved an abrasion wear of less than 0.025mm on concrete not greater than 35N/mm2 with a cement content less than 325kg/m2. 
The floor shall be constructed in a weatherproof structure. 
Apart from saw cutting of induced joints, the floor shall be left undisturbed for 3 full days after construction. 
The main contractor shall provide and maintain protection from any subsequent site operations in this contract.